# Technical Data Sheet

Semigloss Tile Floor Resin

Topcoat Refinishing Paint Component

# Description

You asked about tile floor coating for quite some time – well now, it’s finally here!  Imagine now being able to refinish tile floors without having to worry about scratches from a pebble in your shoe tread or scuffing from your boot heel.  This resin is scratch, mar, and scuff resistant – standing up to the most abusive behavior from your feet!  Fast dry and cure times mean your customers can walk with confidence across their new floor quickly.

# Laboratory Data							Typical Properties

Appearance								Opaque Liquid

Specific Gravity								1.26

Flash Point 								40°F

%N.V. (typical)								59.6

VOC									1.84 lbs./gal											220.5 g/L

Coverage per Gallon at recommended film thickness			200-250 sq. ft.

Total Film Thickness (dry) 						2.5 – 3.5 mil

# Application

For the average size bathroom floor (approximately 70 square feet), mix 14 oz. of Semigloss Tile Floor Resin with 7 oz. of Universal Catalyst (by volume). Thin with 7 oz. of the All-Purpose Reducer to spray apply.  Spray 1 light tack coat followed by 2 heavier coats. Wearing shoe spikes, spray starting from the corner furthest from the door, working backward until you’ve exited the room. Allow the coating to dry to touch before applying the next coat. At 75F and 50% humidity, Semigloss Tile Floor coating will dry to touch in 10-15 minutes.  Unmask and remove tape after the last coat is fully dry to the touch (approximately 25 minutes)

# Surface Preparation

The method recommended by NAPCO is to use the wipe-on primer and bonding agent NAPCO Gorilla Grip, after the tile floor is cleaned with NAPCO Piranha Prep. Refer to the Tech Data Sheets and SDSs for these products.

# Mixing Instructions

The NAPCO Semigloss Tile Floor Resin should be shaken constantly for 15-20 seconds before use. For the average size bathroom floor (approximately 70 square feet), mix 14 oz. of Semigloss Tile Floor Resin with 7 oz. of Universal Catalyst (by volume). Thin with 7 oz. of the All-Purpose Reducer to spray apply.

# Temperature/Humidity Considerations

Application temperatures between 68F and 792 are recommended for best performance.  In general, application at temperatures above 90F will result in reduced pot-life, lower gloss, and sometimes a powdery appearance known as “dry spray”. At temperatures around 50F, the cure and tack times will increase threefold.

# Notes and Precautions

Refer to the SDS sheet before use. The NAPCO Semigloss Tile Floor Resin should be shaken constantly for 15-20 seconds before use. For the average size bathroom floor (approximately 70 square feet), mix 14 oz. of Semigloss Tile Floor Resin with 7 oz. of Universal Catalyst (by volume). Thin with 7 oz. of the All-Purpose Reducer to spray apply.

All components should be stored indoors between 50-90 F. Shelf-life in unopened containers is one year from the date of manufacture. The catalyst is particularly sensitive to high humidity, so the catalyst container must be kept always closed when not in use. The viscosity of the resin will more than double at 50F vs. 75F (perhaps requiring more reducer for proper spray, which further lengthens the recoat tack times as well as slowing down the cure). If the components are stored at high temperatures, (90F and above), the viscosity of the base will noticeably be lowered, and the solvents in the mixed paint will evaporate more rapidly, causing too fast a “dry” and may result in a lower gloss and powdery finish. The shorter pot-life at high temperatures could lead to drastically shortened working time and could even gel in the paint pot.

# Storage

All components should be stored indoors between 50-90 F. Shelf life in unopened containers is one year from the date of manufacture. The catalyst is particularly sensitive to high humidity, so the catalyst container must be kept always closed when not in use.

11/22 - SAZ